Cooper Racing Green as researched by John Cooper, David Cooper and Dupont is

Dupont Chromabase.
Color Spectramaster Green, Value shade #7 

GS 57612 Tinting Guide mixed as follows for a 2 quart pot.

806J HS Black 193.4 grams
830J HS Fast Green 290 grams
881J HS Yellow Oxide 325.6 grams
801J HS White 351.2 grams
150K B/C Balancer 1328 grams 
175K Binder 1722.8 grams

Mix with 7185 S high temp Chroma system basemaker 1:1 for application.

Best results come from using Dupont primer/surfacer 30S Gray as an under coat.